EXPERIMENTAL STUDY ON EFFECT OF RELATIVE COMPACTION AND PERCENT FINES ON THE PERMEABILITY OF SOILS

Ketan Bajaj (1), Yash Shrivastava(2) & B.V.H. Ramakanth(3)

1) Applied Mechanics Department, S.V. National Institute of Technology, Surat, India, 16ketan1990@gmail.com

2) University of Petroleum and Energy Studies, Dehradun, India, yashanshu.shrivastava8@gmail.com

3) NICMAR, Goa, India, bramakanth29@gmail.com

Permeability is the major property of soil that affecting the various engineering aspects. It is one of the indispensable soil properties which are to be taken utmost care in soil problems like settlement of foundations, seepage through and below the earth structures like dams, yields of wells, constructions of highway roads etc. The aim of this research is to reduce the permeability of soil sample by varying the percentage of percent fines and fly ash and then compacted so that the voids present in soils are filled up and the settlement of the structures is reduced. This paper also addresses the effect of percent fines and fly ash on the permeability of the soil. Soil is altered with inclusion of fine content and fly ash in 30%, 40%, 50% 60% & 70% to form different soil mixes. Tests were carried out to determine the index properties, compaction characteristics with changing the height of fall and weight of hammer and permeability of remolded soil. The maximum dry density (MDD) and Optimum Moisture Content (OMC) decreased and increased, respectively with increase in % fines content and fly ash. It is seen that up to 40% fines soil proves better material as percent fines while above 40% fly ash serves as a better percent fines material and reduces permeability to a much greater extent than soil. Thus with the decrease in permeability by the effect of compaction and percent fines the shrinkage risk of the soil is also decreased. Thus the settlement of the structure is decreased.

Keywords: - Permeability, Fly ash, percent fines, Proctor test, settlement

- Introduction

Permeability as we know is the major property of soil involving and affecting the various engineering aspects.it is one of the indispensable part which is to be taken utmost care in engineering problems like settlement of foundations, seepage through and below the earth structures like dams, yields of wells, constructions of highway roads etc. A material is considered porous if it contains interstices. The porous material is permeable if the interstices are interconnected or continuous. A liquid can flow through a permeable material. According to the studies made by the scientists the electron photomicrographs of even very fine clay indicate that the interstices are interconnected. However the size, cross section, and orientation of interstices in different soils are highly variable. In general, studies conclude that all the soils are permeable up to some extent. Permeability as such controls the hydraulic stability of the soil masses.                           Various experimental tests and methods have been developed to decrease the permeability of the soils, thus to improve the soil properties for a better and safer construction.

As the availability of good construction sites are decreasing ground improvement is a rapidly developing field. Decreased permeability to improve soil properties is required to reduce the voids ratio and the water content to increase its strength so that the bearing capacity is increased and the compressibility is decreased. For a lateritic soil to be effective as a barrier material in waste disposal facilities, it is expected to contain appreciable quantities of fines that enable the soil in its compacted state to yield low hydraulic conductivity values (k) generally less than 10-9 m/s. A. Erwandy conclude that the introduction of 40% fines to the mixture causes a very significant reduction in the permeability; there is a less dramatic reduction in permeability with further increase in the amount of fines. At any fines is considerably more permeable than the mixture made with plastic fines. Shanyong Wang found that, as the fines content increases, the dry density decreases, however the optimum water content increases. In addition, the permeability is decreased due to a reduction in void ratio, and the coefficient of consolidation increases with higher fines content. This results in an increase in the viscosity of the pores water thus reducing the flow rate of the fluid. Wen-Yafeng concluded that coefficient of permeability of the soil is seriously influenced by the by compaction efforts and the coefficient of permeability of soft rock remain almost unchanged with the change in compaction effort. B.A. Mir is explained that there is a pronounced decrease in permeability with an increase in dry unit weight at a given water content (OMC) upto MDD. Beyond MDD, the variation of permeability with varying unit weight is less sensitive. It has been seen that for the same void ratio, a specimen compacted dry of optimum and saturated results in a higher permeability (3.24*10-8m/s), whereas the specimen wet of optimum has a lower permeability (5.31*10-9m/s). This is because the soil structure compacted on the dry side of optimum is randomly oriented (flocculated) than in the wet-side of optimum, which has a more parallel particle orientation (dispersed), mainly characterized by long strings with face-to-face contacts between the particles. The aim is to reduce the permeability of soil sample by the effect of percent fines and compaction so that the voids present in soils are filled up and the settlement of the structures reduce.

- Material Used

For the present work, disturbed and undisturbed soil samples were collected from a site at three locations in Dehradun where ground was already excavated to about a depth of 12ft (4mts.) and Class C Fly Ash (FA) which is locally available for the purpose of laying sub-base and base of a road. All the tests were carried out as per the relevant Indian Standards. The chemical properties of FA shown in table 1 and physical properties of materials used are listed in Table 2.

Table 1 Chemical Properties of fly ash used

| Constituent | FA |
| --- | --- |
| Al2O3 | 26.8 |
| SiO2 | 55.3 |
| Fe2O3 | 13.6 |
| CaO | 2.98 |
| MgO | 1.24 |
| Loss on Ignition | 13.3 |

Table 2 Physical properties of material used

| Properties | Values |  |
| --- | --- | --- |
|  | Soil | FA |
| Specific Gravity | 2.64 | 2.36 |
| MDD(g/cc) | 1.84 | 1.23 |
| OMC (%) | 15.5 | 31.2 |
| Liquid Limit (%) | 35.67 | 63.5 |
| Plastic Limit (%) | 25.68 | 46.2 |
| Permeability (m/sec) | 2.14E-07 | 1.5E-04 |
| Angle of internal friction (°) | - | 35 |
| Shear Strength (kPa) | 23.5 | - |
| Unsoaked CBR (%) | 10.32 | 9.25 |
| Soaked CBR (%) | - | 8.82 |

- Experimental Study

The permeability test was performed on the soil having 30%, 40%, 50%, 60% and 70% fines and also with the replacement of soil with 30%, 40%, 50%, 60% and 70% fly ash and firstly maximum dry density (MDD) and optimum moisture content (OMC) and the soil is compacted on MDD in rigid wall compaction mould parameters used in falling head method. This method can measure much smaller volumes of flow. Within a time period, t, a decrease of water level in a volumetric tube with the cross-sectional area, a, from the height h1 to h2 is measured. Tests were run at a constant temperature of 20±1°C. Specimens were placed in a cell and saturated from the bottom until water ponded at the top. Then, the coefficient of permeability, k (m/s) is determined by using the Darcy’s equation:

k=aLA(t1-t2)logeh1h2

where, a = cross-sectional area of the standpipe (m2);

L = length of the soil specimen (m);

A = cross-sectional area of the specimen (m2);

t1 = initial test time (min); t2 = final test time (min);

h1 = initial hydraulic head (m) at time t1; and

h2 = final hydraulic head (m) at time t2.

- Result and Discussions

4.1. Particle size distribution curves

The particle size distribution curves are drawn with soil having 30%, 40%, 50%, 60% and 70% fines and also with the replacement of soil with 30%, 40%, 50%, 60% and 70% fly ash as shown in figure 1 & 2. It has been seem that coefficient of curvature goes on decreasing with the increase in fly ash percent as well as % fines. There is no such change in coefficient of curvature as far as % fines are concerned whereas in case of fly ash it increases with the increase in fly ash content.

Figure 1 Particle size distribution with % fines

Figure 2 Particle size distribution curves with Fly ash

The grading modulus is computed from the following equation

GM=300-%passing 2.4mm+%< 4.75mm+%<75μm100

where, % passing 2.4mm = Percentage of particle sizes passing sieve with 2.4mm aperture; % < 0.425mm = Percentage of particle sizes less than 0.425mm; % < 0.075μm = Percentage of particle sizes less than 0.075mm.

The percentage of % fines increased from 30 to 70%. The relationship between the grading modulus (GM) determined using above eq. and Fig. 3 shows that GM decreases with higher % fines and fly ash content It implies that GM is inversely related to the fines content of the reconstituted soils.

Figure 3 Change in grading modulus with %fines and FA

4.2 Relationship between Atterbergh Limit and %fines and fly ash

The variation of Atterberg limits (i.e., the liquid limit (LL), plastic limit (PL) and plasticity index (PI) of the reconstituted soils with fines and fly ash content is shown in Fig. 4. Generally, the Atterberg limits of the samples obviously increased with higher fines content and this is in agreement with the results reported. The results show that as the amount of fines and fly ash content increased, the resultant specific surfaces and activity of the material also increased that why there is an increase in Atterberg limit values. This was so because the Atterberg limit values were proportional to the specific surfaces provided by the fines content. However, clay soils with too high liquid limit (LL) are more susceptible to desiccation cracking, whereas clay soils with too low plastic limit (PL) and plasticity index (PI) are less workable resulting in a higher probability of the existence of macro pores and poor inter lift bonding. In general soils with very high liquid limit have poor volume stability and high shrink-swell potentials. So, with the increase in % fines and fly ash content soil will become more workable but instead susceptible to crack also.

Figure 4 Atterberg’s Limit with change in %fines

4.2. Relationship between compaction of soil and % fines and fly ash

The Standard Proctor test is adopted to study the effect of fines content on the compressibility of the soil. Fig. 5 & 6 show the compaction curves for soil samples with different fines contents of 30%, 40%, 50%, 60% and 70% fines and also with the replacement of soil with 30%, 40%, 50%, 60% and 70% fly ash by weight. It is found that as the fines content increases, the dry density decreases. However, the optimum water content increases with increase in fines content which is illustrated in Fig. 7.

Figure 5 Compaction curves with % Fines

Figure 6 Compaction curves with Fly ash

A possible explanation for the increase in the optimum water content is due increase in the void ratio in the sample due to higher fines content in the ‘‘dry of optimum” stage. Examining the microstructure of soil, the fine grained particles move randomly in pores space and can intrude into the inter-particles space of larger particles and separate the soil particles apart.. Furthermore, referring to cluster hypothesis by Barden and Sides, the clay particles would form cluster with soil particles and water. These two effects separate the soil particles, formed intra-aggregate, and inter aggregate pores within the soil sample. As a result, the dry density will decrease. In addition, the absorption of water reduces the viscosity of the pore water. Thus, it increases the lubricating effect for rearrangement of soil particles. Accordingly, as the percentage of clay in the sample increases, more clay particles exist in the void of the soil. It tends to absorb water and more water must be added to reach the optimum water content.

Figure 7 Variations of OMC and MDD with % Fines & FA

4.3. Relationship between permeability and % fines and fly ash

Falling-Head tests were carried out to determine the permeability of soils with different fines content. It is shown in Fig. 8 that the permeability declines with increase in the % fines. It is suggested that this relationship is highly non-linear which shows an exponential relationship. Fig. 9 shows the plot of fines content against log K as a linear relationship. The permeability decreased gradually with fines content and fly ash content increased could be explained by the fact that fine particles are being suspended in the pores water and they moved along the flow path. This results in an increase in the viscosity of the pores water thus reducing the flow rate of the fluid.

Figure 8 change in permeability coefficient with % fines and FA

Figure 9 change in permeability coefficient with % fines and FA

4.4 Relationship between compaction efforts upon permeability

The test was conducted with percent different values of hammer as 2.495 and 4.54 kg with different number of blow variation as 25, 50 and 70. The coefficient of permeability 45% in case of % fines contents as 70% and number of blows as 74 as compare to weight of hammer. Similarly in case of fly ash content there is approximately 60% increase in the permeability co-efficient with the increase of fly ash content to 70%.

Also it has been seen with increase in number of blows and taking weight of hammer as same the permeability coefficient changes a little bit as there is less increment in MDD and decrement in OMC as shown in table 3 & 4 (in appendix A)

- CONCLUSION

It is seen that up to 40% fines soil proves better material as percent fines while above 40% i.e. 50% and above fly ash serves as a better percent fines material and reduces permeability to a much greater extent than soil. Thus with the decrease in permeability by the effect of compaction and percent fines the shrinkage risk of the soil is also decreased. Thus the settlement of the structure is decreased. Fly ash stands to be more effective as percent fines than sieved soil as seen from the results. Fly ash is more economical than soil as no labor work is required for sieving it.

It has been seem that coefficient of curvature goes on decreasing with the increase in fly ash percent as well as % fines. There is no such change in coefficient of curvature as far as % fines are concerned whereas in case of fly ash it increases with the increase in fly ash content and GM decreases approximately 5 to 10 % with every 10% increase in % fines and fly ash content. So, with the increase in % fines and fly ash content soil will become more workable but instead susceptible to crack also.

It is found that as the fines content increases, the dry density decreases. However, the optimum water content increases with increase in fines content and fly ash content. It is also seem that there is highly non-linear relationship with the increment of fly ash and % fines content. It can be also concluded that with the increase in percent fines up to 60% showing a good result as far as OMC and MDD and permeability all together is concerned but with the 40% of fly ash we could get approximately same result as that of 60% of fly ash content. So, Fly ash is more economically as it’s a by-product and also easily available at reasonable rates.

- References

Indian Codes

- IS: 2720-part 1 (1980), Indian Standard Code for preparation of soil samples, Bureau of Indian Standards, New Delhi.

- IS: 2720-part 4 (1985), Method of test for soils: Determination of grain size distribution, Bureau of Indian standards, New Delhi.

- IS: 2720-part 5 (1985), Method of test for soils: Determination of Atterberg limits, Bureau of Indian standards, New Delhi.

- IS: 1498 (1970). Method of test for soils: Classification and identification of soils for general engineering purposes, Bureau of Indian standards, New Delhi.

- IS: 2720-part 7 (1980), Method of test for soils: Determination of compaction characteristics, Bureau of Indian standards, New Delhi.

- IS: 2720-part 17 (1986), Method of test for soils: Determination of permeability, Bureau of Indian standards, New Delhi.

Journals

- Mitchell, J.K., Hooper, D.R., and Campanella, R.G.(1965), Permeability of compacted clay, Jl. of Soil Mech. Fd., Divn., ASCE, Vol. 91, No. SM4, pp. 41-65.

- Kim D, Sagong M, Lee Y. Effects of fine aggregate content on the mechanical properties of the compacted decomposed granitic soils. Construct Build Mater 2005;19:189–96.

- Augusta E. (2000) The Influence of Fines Content and Plasticity on the Strength and Permeability of Aggregate Base Class A, Thesis, Master Program on Highway and Development, Bandung Institute of Technology

Books

- Lambe, T. W. (1958), The engineering behaviour of compacted clay, Jl. of Soil Mech. and Fd. Divn., Vol. 84, No. SM 2, pp. 1655-1 to 1655-35.

- Peck, R.B., Hanson, W.E. and Thornburn, T.H. Foundation Engineering. 2nd Ed. John Wiley and Sons Inc., New York, 1974.

APPENDIX A

Where F=% fines and FA=Fly ash

Table 3 Change in permeability coefficient with number of blows when hammer weight is 2.495 kg

| Sample | % Fines and FA | Hammer Weight (Kg) | Number of blows | MDD (g/cc) | OMC (%) | Permeability Coefficient (m/sec) |
| --- | --- | --- | --- | --- | --- | --- |
| F1 | 30 | 2.495 | 25 | 1.79 | 17.63 | 5.26 E-07 |
|  |  |  | 50 | 2.00 | 17.50 | 5.25 E-07 |
|  |  |  | 75 | 2.05 | 17.50 | 5.20 E-07 |
| F2 | 40 | 2.495 | 25 | 1.75 | 18.50 | 4.65 E-07 |
|  |  |  | 50 | 1.78 | 18.45 | 4.60 E-07 |
|  |  |  | 75 | 1.79 | 18.41 | 4.55 E-07 |
| F3 | 50 | 2.495 | 25 | 1.73 | 18.90 | 4.25 E-07 |
|  |  |  | 50 | 1.745 | 18.85 | 4.21 E-07 |
|  |  |  | 75 | 1.76 | 18.82 | 4.19 E-07 |
| F4 | 60 | 2.495 | 25 | 1.70 | 19.25 | 3.82 E-07 |
|  |  |  | 50 | 1.72 | 19.23 | 3.75 E-07 |
|  |  |  | 75 | 1.75 | 19.22 | 3.62 E-07 |
| F5 | 70 | 2.495 | 25 | 1.69 | 20.00 | 3.25 E-07 |
|  |  |  | 50 | 1.70 | 19.98 | 3.14 E-07 |
|  |  |  | 75 | 1.71 | 19.97 | 3.05 E-07 |
| FA1 | 30 | 2.495 | 25 | 2.00 | 16.32 | 8.00 E-07 |
|  |  |  | 50 | 2.05 | 16.27 | 7.95 E-07 |
|  |  |  | 75 | 2.10 | 16.25 | 7.94 E-07 |
| FA2 | 40 | 2.495 | 25 | 1.95 | 17.22 | 5.41 E-07 |
|  |  |  | 50 | 1.98 | 17.18 | 5.35 E-07 |
|  |  |  | 75 | 2.04 | 17.15 | 5.31 E-07 |
| FA3 | 50 | 2.495 | 25 | 1.90 | 18.00 | 4.03 E-07 |
|  |  |  | 50 | 1.93 | 17.98 | 3.96 E-07 |
|  |  |  | 75 | 1.96 | 17.95 | 3.89 E-07 |
| FA4 | 60 | 2.495 | 25 | 1.80 | 19.20 | 2.94 E-07 |
|  |  |  | 50 | 1.84 | 19.18 | 2.85 E-07 |
|  |  |  | 75 | 1.87 | 19.15 | 2.72 E-07 |
| FA5 | 70 | 2.495 | 25 | 1.74 | 19.70 | 2.33 E-07 |
|  |  |  | 50 | 1.78 | 19.68 | 2.23 E-07 |
|  |  |  | 75 | 1.79 | 19.67 | 2.15 E-07 |

Table 4 Change in permeability coefficient with number of blows when hammer weight is 4.54 kg

| Sample | % Fines and FA | Hammer Weight (Kg) | Number of blows | MDD (g/cc) | OMC (%) | Permeability Coefficient (m/sec) |
| --- | --- | --- | --- | --- | --- | --- |
| F1 | 30 | 4.54 | 25 | 1.82 | 17.60 | 4.36 E-07 |
|  |  |  | 50 | 2.10 | 17.45 | 4.35 E-07 |
|  |  |  | 75 | 2.12 | 17.45 | 4.30 E-07 |
| F2 | 40 | 4.54 | 25 | 1.79 | 18.39 | 3.56 E-07 |
|  |  |  | 50 | 1.82 | 18.36 | 3.06 E-07 |
|  |  |  | 75 | 1.83 | 18.33 | 3.54 E-07 |
| F3 | 50 | 4.54 | 25 | 1.77 | 18.81 | 3.15 E-07 |
|  |  |  | 50 | 1.79 | 18.81 | 3.11 E-07 |
|  |  |  | 75 | 1.81 | 18.81 | 3.09 E-07 |
| F4 | 60 | 4.54 | 25 | 1.76 | 19.15 | 2.72 E-07 |
|  |  |  | 50 | 1.78 | 19.13 | 2.58 E-07 |
|  |  |  | 75 | 1.79 | 19.12 | 2.49 E-07 |
| F5 | 70 | 4.54 | 25 | 1.71 | 19.95 | 2.28 E-07 |
|  |  |  | 50 | 1.73 | 19.94 | 2.19 E-07 |
|  |  |  | 75 | 1.74 | 19.94 | 2.08 E-07 |
| FA1 | 30 | 4.54 | 25 | 2.02 | 16.22 | 7.08 E-07 |
|  |  |  | 50 | 2.08 | 16.17 | 6.75 E-07 |
|  |  |  | 75 | 2.13 | 16.15 | 6.74 E-07 |
| FA2 | 40 | 4.54 | 25 | 2.01 | 17.12 | 4.38 E-07 |
|  |  |  | 50 | 2.03 | 17.08 | 4.32 E-07 |
|  |  |  | 75 | 2.04 | 17.05 | 4.29 E-07 |
| FA3 | 50 | 4.54 | 25 | 2.00 | 17.92 | 3.06 E-07 |
|  |  |  | 50 | 2.05 | 17.88 | 2.76 E-07 |
|  |  |  | 75 | 2.05 | 17.85 | 2.79 E-07 |
| FA4 | 60 | 4.54 | 25 | 1.90 | 19.10 | 1.84 E-07 |
|  |  |  | 50 | 1.94 | 19.08 | 1.76 E-07 |
|  |  |  | 75 | 1.97 | 19.05 | 1.69 E-07 |
| FA5 | 70 | 4.54 | 25 | 1.85 | 19.65 | 1.10 E-07 |
|  |  |  | 50 | 1.89 | 19.62 | 1.05 E-07 |
|  |  |  | 75 | 1.90 | 19.60 | 9.98 E-08 |